## 4.

## 4.1. Recommended Number of Composite Layers for Bending Stiffness & Minimum Weight

- Minimum Required Layers:

  - 3-ply layup (~0.53 mm thickness) was identified as the minimum requirement to prevent porosity and moisture intrusion​.[8]

  - Hybrid CFRP-GFRP composite laminates were found to be 17% lighter while maintaining stiffness​.

- Optimal Layer Count for Stiffness vs. Weight Trade-off:

  - 36–40 layers were recommended for fuselage structures under bending and impact loads​.

  - Unidirectional laminates with [0]12 performed best in flexural strength but were prone to brittle failure​.[9]

- Impact on Performance & Cost:

  - DD layup ([±30°/90°/0°/±75°]) provided higher torsional stiffness and weight efficiency than traditional stacking sequences​.

  - Multi-objective optimization showed that minimizing layers reduced weight, but at the cost of lower impact resistance​.[10]

### Comparison Across Papers:

Study; Optimal Layer Count; Weight Savings; Comments. Minimum Cost & Weight Design​; 3-ply min; Moderate; Manufacturing constraints require a minimum of 3 plies. Optimal Layup Selection​; 36-40 layers; High; DD layups outperformed traditional sequences. Kevlar-Glass Fiber Laminates​; 6 layers; Moderate; Kevlar improved impact resistance but didn’t enhance stiffness. Stacking-Sequence Design​; Computed via optimization; High; Symmetric stacking reduced stress concentrations. Numerical Optimization​; Hybrid CFRP-GFRP; 17% weight reduction; Reduced weight while maintaining impact tolerance.

## 4.2. Relation Between the Number of Layers & Fuselage Stiffness Under Bending

- Thicker laminates increase bending stiffness, but excessive layers lead to stress concentrations and premature delamination​.[8]

- Hybrid laminates provided a 17% weight reduction while maintaining stiffness, making them ideal for aerospace fuselages​.

- Pareto frontier optimization showed that fewer layers improve cost-effectiveness but reduce flexural resistance​.

- Shear failures were observed in unidirectional laminates ([0]12), emphasizing the need for multidirectional layups​.[9]

### Comparison Across Papers:

Study; Effect of More Layers; Key Findings. Minimum Cost & Weight Design​; Stiffness ↑, Stress ↑; More layers increase stiffness but require symmetric stacking to avoid stress concentrations. Optimal Layup Selection​; Stiffness ↑, Weight ↑; Balanced laminates offer the best trade-off between stiffness and weight. Kevlar-Glass Fiber Laminates​; Stiffness ~; Kevlar improved toughness but had minimal effect on bending stiffness. Stacking-Sequence Design​; Stiffness ↑; Gradual ply transitions improve stiffness while reducing stress concentrations. Numerical Optimization​; Stiffness ↑; Weight-efficient hybrid laminates showed better performance than CFRP-only laminates.

## 4.3. Optimal Fiber Orientation for Cylindrical Composite Fuselage Under 3-Point Bending

- Best Ply Orientations for Bending:

  - 0° plies improved axial stiffness but increased delamination risk​.

  - ±45° plies significantly improved impact absorption and shear strength​.[9]

  - 90° plies enhanced lateral stability but contributed minimally to bending stiffness​.[10]

- Key Findings by Orientation:

  - 0° Unidirectional Laminates ([0]12) → High stiffness but brittle failure​.

  - ±45° Laminates ([±45]3s) → Best impact absorption and damage tolerance​.

  - Multidirectional Laminates ([0/90/(±45)2s]) → Best balance between impact resistance and bending stiffness​.

### Comparison Across Papers:

| Ply Orientation | Best For | Study |
| --- | --- | --- |
| 0° (Axial Load-Bearing) | Maximum stiffness, but brittle failure | Stacking-Sequence Design​ |
| ±45° (Shear Strength & Energy Absorption) | Best for impact and fatigue resistance | Effect of Stacking Sequence​ |
| 90° (Transverse Stability) | Improves lateral stability, but limited bending stiffness | Kevlar-Glass Hybrid Study​ |
| DD Layup ([±30°/90°/0°/±75°]) | Best torsional stiffness & weight efficiency | Optimal Layup Selection​ |

## 4.4. Recommendations on Symmetric & Balanced Layups for Stress Reduction & Delamination Prevention

- Symmetric and balanced laminates ([0°/±45°/90°]2s) provided the best damage resistance and weight optimization​.

- Multidirectional layups improved energy absorption, making them ideal for fuselage cutouts and areas prone to stress concentration​.

- Hybrid CFRP-GFRP laminates reduced interlaminar stress while maintaining bending stiffness​.

Optimization Plan for SAMPE Fuselage Layup

Step 1: Define Objectives

- Maximize bending stiffness to minimize deflection under a 1,000 lbf load.

- Minimize interlaminar shear stress to prevent delamination around cutouts.

- Optimize weight while maintaining structural integrity.

Step 2: Constraints

- Symmetry: Ensure symmetric stacking sequence to avoid warping.

- Balance: Include equal numbers of +45° and -45° plies for torsional stability.

- Minimum Ply Count: At least three plies per orientation (0°, ±45°, 90°).

Step 3: Candidate Layup Configurations

| Layup Configuration | Description | Expected Performance |
| --- | --- | --- |
| [0/90/(±45)₂s] | Symmetric, balanced multidirectional layup | Best balance between bending stiffness, shear strength, and damage tolerance. |
| [±45/0]₆ | Double-biaxial angle layup | High shear strength but reduced axial stiffness compared to multidirectional layups. |
| ₁₂ | Unidirectional layup | High axial stiffness but prone to brittle failure under transverse loads. |

Step 4: Evaluate Performance Using Classical Lamination Theory (CLT)

- Calculate laminate stiffness matrix (DD) for each configuration:

D=112∑k=1nQk⋅(zk3−zk−13)D=121k=1∑nQk⋅(zk3−zk−13)

Where QkQk is the transformed reduced stiffness matrix for each ply orientation.

- Analyze shear stress distribution under applied loads:

τxy=VA+stress concentration factors near cutoutsτxy=AV+stress concentration factors near cutouts

- Use Tsai-Wu failure criterion to predict failure modes:

F1σx+F2σy+F11σx2+F22σy2+F12σxσy+F66τxy2=1F1σx+F2σy+F11σx2+F22σy2+F12σxσy+F66τxy2=1

Step 5: Perform Multi-Objective Optimization

Use optimization software (e.g., MATLAB or ANSYS):

- Define objectives:

  - Maximize D11D11 (axial stiffness).

  - Minimize peak shear stress (τxyτxy).

  - Minimize weight (ttotalttotal).

- Apply constraints:

  - Symmetry and balance.

  - Minimum ply count per orientation.

- Run optimization algorithms:

  - Genetic Algorithm (GA): Explore global optima for stacking sequences.

  - Branch-and-Bound: Efficiently refine stacking sequences within manufacturing constraints.

Final Deliverable

Once optimized, validate the selected layup using Finite Element Analysis (FEA) to confirm:

- Compliance with SAMPE load-deflection requirements (≤≤1" deflection under 1,000 lbf).

- Reduced shear stress concentrations around cutouts.